SYNTHESIS AND INVESTIGATION OF PPG BASED ON POLYACRYLAMIDE TO REDUCE WATER CUT IN OIL WELLS

Yelemessova G.T.1*, Klivenko A.N. 1, Orazzhanova L.K.1, Sabitova A.N.1, 
Shakhvorostov A.V.2, Aseyev V.O.3

*E-mail: kussainova_g91@mail.ru

Table S1. Mass of reagents for the synthesis of hydrogels with a change in the concentration of the crosslinking agent

| Concentration of crosslinking agent, % | 1 | 2 | 3 | 4 | 5 |
| --- | --- | --- | --- | --- | --- |
| Composition of the initial monomer mixtures | Mass, g |  |  |  |  |
| Bentonite | 0.5 | 0.5 | 0.5 | 0.5 | 0.5 |
| Water | 9 | 9 | 9 | 9 | 9 |
| MBAA | 0.0054 | 0.008 | 0.0212 | 0.0364 | 0.0511 |
| AAm | 0.4491 | 0.4466 | 0.4347 | 0.4209 | 0.4070 |
| SA | 0.0455 | 0.0453 | 0.0441 | 0.0427 | 0.0419 |

Table S2. The asses of reagents for the synthesis of hydrogels of the AAm/SA monomer ratio

| Ratio Aam/SA, % | 95/5 | 90/10 | 85/15 | 80/20 | 75/25 |
| --- | --- | --- | --- | --- | --- |
| Composition of the initial monomer mixtures | Mass, g |  |  |  |  |
| Bentonite | 0.5 | 0.5 | 0.5 | 0.5 | 0.5 |
| Water | 9 | 9 | 9 | 9 | 9 |
| MBAA | 0.0107 | 0.0107 | 0.0107 | 0.0107 | 0.0107 |
| AAm | 0.4645 | 0.4151 | 0.4068 | 0.3903 | 0.2430 |
| SA | 0.0248 | 0.0742 | 0.0825 | 0.0990 | 0.2464 |

Table S3. Masses of reagents for the synthesis of hydrogels with a change in bentonite concentration

| Concentration of bentonite, % | 5 | 10 | 15 | 20 | 25 |
| --- | --- | --- | --- | --- | --- |
| Composition of the initial monomer mixtures | Mass, g |  |  |  |  |
| Bentonite | 0.1 | 0.2 | 0.3 | 0.4 | 0.5 |
| Water | 9.4 | 9.3 | 9.2 | 9.1 | 9 |
| MBAA | 0.0107 |  |  |  |  |
| AAm | 0.4442 |  |  |  |  |
| SA | 0.045 |  |  |  |  |